ARCHITECTURAL SUBMITTAL LETTER

Date: ___________________

To Whom It May Concern,

This letter confirms the performance testing and ASTM compliance of the following King Klinker thin brick products:

- White Clay Body

- Brown Clay Body

- Red Clay Body

All products were independently tested by Clemson University’s Bishop Materials Laboratory in accordance with ASTM C67 Standard Test Methods. Test results were evaluated against ASTM C1088-24 Standard Specification for Thin Veneer Brick Units.

ASTM Compliance

The tested products comply with:

- ASTM C1088-24, Grade Exterior

- Types TBX and TBS

- Requirements for absorption, efflorescence, dimensional tolerances, and warpage

Key Performance Results:

- Ultra-low absorption: 1.1%–3.5% (well below ASTM limits)

- Efflorescence: None observed

- Dimensional accuracy: Meets ASTM TBX tolerances

- Warpage: 0–2/32", within TBX limits

- Durability: Suitable for all North American climates

These results confirm that King Klinker thin brick products meet the physical property requirements for use in exterior and interior architectural applications, including adhered veneer systems, panelized façades, and traditional masonry installations.

If additional documentation or technical support is required, please contact King Klinker Thin Brick.

Sincerely,

King Klinker Thin Brick
300 Sherry Lynn Lane
Sparta, WI 54656
Phone: 608-317-3265