STATEMENT OF COMPLIANCE

King Klinker Thin Brick Products
White Clay • Brown Clay • Red Clay
Tested by Clemson University – Bishop Materials Laboratory

ASTM Compliance Certification

This Statement of Compliance confirms that the thin brick products listed above have been independently tested in accordance with ASTM C67 Standard Test Methods for Sampling and Testing Brick and Structural Clay Tile, and evaluated against the requirements of ASTM C1088-24 Standard Specification for Thin Veneer Brick Units Made From Clay or Shale.

Based on the completed testing, the products listed demonstrate full compliance with the following ASTM classifications:

- ASTM C1088-24 — Grade Exterior

- ASTM C1088-24 — Type TBX and TBS

- ASTM C67 — Sampling and Physical Property Testing

Verified Performance Criteria

All products meet or exceed the following ASTM physical property requirements:

- Absorption: 1.1%–3.5%, significantly below ASTM limits

- Efflorescence: No efflorescence observed

- Dimensional Tolerances: Meets TBX (tightest ASTM classification)

- Warpage: 0–2/32", within TBX limits

- Saturation Coefficient: Not required (all absorption values < 8%)

These results confirm the suitability of King Klinker thin brick for use in exterior and interior architectural applications, including adhered masonry veneer systems, rainscreen assemblies, panelized systems, and traditional thin brick installations.

Compliance Statement

All tested King Klinker thin brick products are in full compliance with ASTM C1088-24, Grade Exterior, Types TBX and TBS, and are approved for use in accordance with applicable building codes and industry standards governing thin masonry veneer systems.

Third-Party Verification

Testing was conducted by:

Clemson University – Bishop Materials Laboratory
Anderson, South Carolina
An accredited, independent testing facility following ASTM standards.

Authorized By

King Klinker Technical Services
300 Sherry Lynn Lane
Sparta, WI 54656
Phone: 608-317-3265