KING KLINKER THIN BRICK – ASTM PERFORMANCE REVIEW

Products Tested: White Clay Body, Brown Clay Body, Red Clay Body

Testing Laboratory: Clemson University – Bishop Materials Laboratory
Test Methods: ASTM C67
Specification Standard: ASTM C1088-24 (Grade Exterior, Types TBX/TBS)

1. Overview

King Klinker thin brick products were independently tested to verify compliance with ASTM C1088-24 requirements for Exterior Grade thin veneer brick. All units were tested in accordance with ASTM C67, which covers sampling and physical property testing for clay brick.

All products passed every applicable ASTM requirement, demonstrating high density, exceptional durability, and excellent dimensional stability.

2. Summary of Key Test Results

Water Absorption (ASTM C67)

| Product | 24-Hr Absorption | 5-Hr Boil Absorption |
| --- | --- | --- |
| White Clay Body | 3.2% | 3.5% |
| Black Clay Body | 1.1% | 1.6% |
| Red Clay Body | 2.4% | 2.6% |

ASTM Requirement:

- ≤ 5% (24 hr)

- ≤ 5% (boiling)
Result: All products significantly outperform ASTM limits.

Saturation Coefficient

Range: 0.70 – 0.94

ASTM Requirement:
Not required for units with < 8% water absorption.
All products fall below 8%.

Efflorescence

All units tested: No efflorescence observed

ASTM Requirement: Must be “Not Effloresced”

Dimensional Compliance & Warpage

- All products meet ASTM TBX dimensional tolerances (tightest classification).

- Warpage ranged from 0–2/32", within TBX limits.

3. Compliance Statement

All tested King Klinker thin brick products meet the physical property requirements of ASTM C1088-24, Grade Exterior, Types TBX and TBS, and are approved for use in adhered veneer systems, panelized façade systems, and traditional masonry applications.

4. Testing Laboratory

All testing was conducted by:

Clemson University
Bishop Materials Laboratory
Anderson, South Carolina

Independent third-party verification ensures accuracy and compliance with ASTM procedures.