PCI Specification for Embedded Clay Thin Brick

Effective May 4, 2016

A. Thin Brick

1. Thickness not less than ½ in. (13mm) nor more than 1 in. (25mm)

2. Face size: 	Modular: 2-1/4 in. (57mm) high by 7-5/8 in. (190mm) long

Norman: 2-1/4 in. (57mm) high by 11-5/8 in. (290mm) long

Closure modular: 3-5/8 in. (90mm) high by 7-5/8 in. (190mm) long

Utility: 3-5/8 in. (90mm) high by 11-5/8 in. (290mm) long

3. Size, color, texture: [Match Architect’s approved samples] [Match existing

adjacent brickwork]

4. [Insert information on existing brick if known]

5. Special shapes: Include corners, edge corners, and end edge corners

6. Back surface texture: [Scored] [Combed] [Wire roughened] [Ribbed]

[Keybacked] [Dovetailed]

B. Dimensional Tolerances – measure in accordance with ASTM C67

1. Thickness: Plus 0 in., minus 1/16 in. (+0, -1.6mm)

2. Face size: Plus 0 in., minus 1/16 in. for dimensions 8 in. (200mm) or less

Plus 0 in., minus 3/32 in. (+0, -2.4mm) for dimensions greater than

8 in. (200mm)

3. Warpage: not more than 1/16 in. (1.6mm) either concave or convex from a

consistent plane

4. Out of square: Plus or minus 1/16 in. (±1.6mm)

5. Shape angle: Plus or minus 1 degree from specified angle

C. Properties

1. Breaking strength: Not less than 250 psi (1.7 MPa) tested in accordance

with ASTM C67

2. Cold water absorption: Maximum 6% at 24 hours tested in accordance with ASTM

C67

3. Efflorescence: Rated “not effloresced” when tested in accordance with ASTM C67

4. Freeze thaw resistance:

a. Uncoated brick: No detectable deterioration (spalling, cracking, or

breaking) after 300 cycles tested in accordance with ASTM C666, Method

A or B on assembled specimens

b. Surface coloring: No observable difference in the applied finish when

viewed at a distance of 20 ft (6m) after 50 cycles tested in accordance with

ASTM C67. In addition, the brick shall undergo ASTM C666 test described

above

5. Pull-out strength: Not less than 150 psi (1.0 MPa) from base concrete before and

after freeze thaw testing tested in accordance with specified modification to

ASTM E488.

6. Chemical resistance: Rated “not affected” when tested with a 10% hydrochloric

acid solution in accordance with ASTM C650.

D. Testing requirements:

1. Minimum number of test specimens: In accordance with appropriate ASTM

specifications except as specified in D.1.a.

a. Exception for freeze thaw and pull-out strength tests: Ten (10) assembled

specimens measuring 8 in. by 16 in. (200mm by 405mm) long with the

brick embedded into the concrete substrate (assembled specimens). The

ten (10) assembled specimens are divided into five (5) Sample A

assemblies and five (5) Sample B assemblies. The precast concrete

substrate shall have a minimum thickness of 2-1/2 in. (63mm) plus the

embedded brick thickness. The precast concrete shall have a minimum

compressive strength of at least 5000 psi (34.5 MPa) and 4 to 6% entrained

air. The embedded brick coursing pattern for testing purposes shall be

modular size brick on a half running bond pattern with a formed raked

joint geometry of no less than 3/8 in. (9mm) wide and a depth no greater

than 1/4 in. (6mm) from the exterior face of the brick.

One brick from the center of each sample assembly shall be tested for pull-

out strength. Each Sample B assembly shall first be tested for freeze thaw

resistance. In place of anchor specified in ASTM E488, use 3/8 in. (9mm)

minimum thickness steel plate of same size as single brick face bonded

with epoxy to a single brick face for each pull-out strength test. The steel

plate shall have a centrally located pull-rod welded to the plate.

2. Back surface texture of samples for pull-out strength and freeze thaw resistance

testing shall be the same.

3. Frequency of testing:

a. Dimensional tolerances shall be checked prior to shipping on each run of

brick supplied to the project.

b. Cold water 24 hour absorption testing shall be conducted on every clay

body/color of project specific brick prior to each shipment. Submit written

documentation. The buyer reserves the right to conduct the same test

prior to first shipment.

c. All other tests specified shall be conducted for each clay body at an

accredited laboratory at least every six years.